Full Data Set.

Notes:

Liquid water saturation calculated assuming 20% linear compression of the GDL material. Uncompressed GDL thickness is 420 micron with 84 % porosity, (compressed is 336 micron with 80% porosity).

For liquid water analysis the cell is divided into 9 sections reaching from the inlets to the outlets In approximately co-flow along the channel.

Liquid water saturation values are the average liquid water saturation in combined anode and cathode GDLs. Section 1 is at the inlet, section 9 is the outlet.

Zero anode inlet Relative humidity, and varying Cathode inlet RH.

Data Set 1:

Data Set 2

Data set 3:

Data set 4: